## Slide 1
Problems | Loss | Reference
1. Mach-Zehnder Modulator (MZM) | 10 to 30 dB/cm (for Depleted PN-junction) | Rahim A, Hermans A, Wohlfeil B, Petousi D, Kuyken B, Van Thourhout D, Baets R. Taking silicon photonics modulators to a higher performance level: state-of-the-art and a review of new technologies. Advanced Photonics. 2021 Mar 1;3(2):024003-.
2. Ring Resonator Add-Drop Filter | 1.3 dB (drop port) | Mirza A, Gloekler RE, Thompson J, Pasricha S, Nikdsast M. Experimental analysis of adiabatic silicon photonic microring resonators under process variations. IEEE Photonics Technology Letters. 2024 Jan 29;36(6):417-20.
3. Dual-Ring Resonator Tunable Filter | 3 dB | 
4. 4-Channel WDM using Cascaded MZIs | 0.45 dB | Yi Q, Zheng S, Yan Z, Cheng G, Xu F, Li Q, Shen L. Silicon photonic flat-top WDM (de) multiplexer based on cascaded Mach-Zehnder interferometers for the 2 µm wavelength band. Optics Express. 2022 Jul 15;30(15):28232-41.
5. Tunable 1×4 Optical Switch | 5.3 dB | Ghanaatian Z, Shafiee A, Nikdast M. Enhanced silicon photonic switch fabrics with variation-aware optimized Mach-Zehnder interferometers. InSilicon Photonics XX 2025 Mar 20 (Vol. 13371, pp. 45-51). SPIE.
6. Balanced Coherent Receiver | 6.5 dB | Sun W, Cao H, Xie J, Xiang Y, Chen T, Guo J, Li H, Yu Z, Dai D. Ultralow-LO-Power Silicon Photonic Coherent Receiver with Balanced Ge/Si Avalanche Photodiodes. ACS Photonics. 2025 Mar 11;12(4):1793-801.
7. 16-Channel AWG | 2.2 dB | Shen X, Li C, Zhao W, Li H, Shi Y, Dai D. Ultra‐Low‐Crosstalk Silicon Arrayed‐Waveguide Grating (De) multiplexer with 1.6‐nm Channel Spacing. Laser & Photonics Reviews. 2024 Jan;18(1):2300617.
8. 2×2 Thermo-Optic Switch | 0.7 dB | Zhang L, Yang T, Zhang E, Zhang S, Yang S, Yang X. Single-stage 2× 2 silicon thermo-optic switch with crosstalk<− 35 dB over 40 nm and Pπ< 8 mW.
9. Y-Branch Power Splitter | 0.28 dB | Zhang Y, Yang S, Lim AE, Lo GQ, Galland C, Baehr-Jones T, Hochberg M. A compact and low loss Y-junction for submicron silicon waveguide. Optics express. 2013 Jan 11;21(1):1310-6.
10. 90-Degree Optical Hybrid | 1.1 dB | Chen Y, Xie X, Sun Y, Pan W, Yan L. Compact optical 90° hybrid based on a wedge-shaped 2× 4 MMI coupler and a 2× 2 MMI coupler on a thin-film lithium niobate platform. Optics Letters. 2024 Feb 20;49(5):1145-8.
11. Add-Drop Multiplexer (OADM) | The same as Add-Drop MRR Filter. | 
12. Tunable Ring Resonator Bank (4 Rings) | 0.08 dB | Sunny F, Shafiee A, Charbonnier B, Nikdast M, Pasricha S. Comet: a cross-layer optimized optical phase-change main memory architecture. In2024 Design, Automation & Test in Europe Conference & Exhibition (DATE) 2024 Mar 25 (pp. 1-6). IEEE.
13. 16-QAM Modulator | The same as Add-Drop MRR Filter. | 
14. Wavelength Selective Switch (1×8) | 5.56 dB | Cheng J, Zhang D, Zeng G, Zhou M, Ding Y, Yin Y. Low-loss and broadband 1× 8 thermo-optic selective switch using bent directional couplers. Results in Optics. 2025 Sep 12:100891.
15. Grating Coupler Array (8 Channels) | Loss per GC : 8 dB | Almeida D, Lourenço P, Fantoni A, Costa J, Vieira M. Grating coupler design for low-cost fabrication in amorphous silicon photonic integrated circuits. InPhotonics 2024 Aug 23 (Vol. 11, No. 9, p. 783). MDPI.
16. Integrated Balanced Photodetector | N/A | 
17. Microring Modulator with Feedback | The same as Add-Drop MRR Filter. | 

## Slide 2
Problems | Loss | Reference
18. 2×2 Switch (PCM‑based) | 2 dB | Chen R, Fang Z, Froch JE, Xu P, Zheng J, Majumdar A. Broadband nonvolatile electrically controlled programmable units in silicon photonics. ACS Photonics. 2022 May 6;9(6):2142-50.
19. 16 × 16 Switch Based on Dual-Ring-Assisted MZI | 10.6 dB | Guo Z, Lu L, Zhou L, Shen L, Chen J. 16× 16 silicon optical switch based on dual-ring-assisted Mach–Zehnder interferometers. Journal of Lightwave Technology. 2017 Sep 13;36(2):225-32.
20. optical delay line | 0.08 dB/m | Lee H, Chen T, Li J, Painter O, Vahala KJ. Ultra-low-loss optical delay line on a silicon chip. Nature communications. 2012 Jan;3(1):867.
Components | Loss | Reference
Multimode Interference coupler (MMI) 1X2 | 0.3 dB | Zhu Z, Zhong Y, Lin D, Tong X, Zhong Q, He J. Low-loss and broadband arbitrary ratios 1× 2 power splitter based on asymmetrically tapered multimode interference. Journal of Optics. 2024 May 21;26(7):075801.
MMI 1X4 | 0.58 dB | Hong S, Yoon J, Kim J, Kim JY, Neseli B, Yoon H, Park HH, Kurt H. Design of MMI-based 1x4 power splitters with optimized parabolic input and output ports on SOI platform. InSilicon Photonics XVIII 2023 Mar 13 (Vol. 12426, pp. 30-35). SPIE.
Y-branch | 0.28 dB | Zhang Y, Yang S, Lim AE, Lo GQ, Galland C, Baehr-Jones T, Hochberg M. A compact and low loss Y-junction for submicron silicon waveguide. Optics express. 2013 Jan 11;21(1):1310-6.
Directional Coupler (DC) | 0.27 dB | Lv D, Wu L, Liu C, Li A, Wang R, Wu A. Broadband and low-loss silicon photonic directional coupler for signal power tapping on the 3 μm soi waveguide platform. InPhotonics 2023 Jul 4 (Vol. 10, No. 7, p. 776). MDPI.
Propagation in waveguides | 0.7 dB/cm | AIM Photonics, “Base passive photonic integrated circuit (PIC) process,” (2024).
Phase Shifters | 0.23 dB | Ding F, Dai J, Chen Y, Zhu J, Jin Y, Bozhevolnyi SI. Broadband near-infrared metamaterial absorbers utilizing highly lossy metals. Scientific reports. 2016 Dec 21;6(1):39445.
Bend | 0.086 dB (Bending Radius = 1µm) | Vlasov YA, McNab SJ. Losses in single-mode silicon-on-insulator strip waveguides and bends. Optics express. 2004 Apr 19;12(8):1622-31.
Taper | 0.016 dB | Shen H, Fan L, Wang J, Wirth JC, Qi M. A taper to reduce the straight-to-bend transition loss in compact silicon waveguides. IEEE Photonics Technology Letters. 2010 May 24;22(15):1174-6.
Waveguide Crossing | 0.03 dB | Lu W, Shi H, Ma C, Li Z, Zhu S, Wu Y, Tai R. Ultra-low loss SOI waveguide crossings designed by a hybrid global optimization based on deep learning. Optics Communications. 2024 Apr 1;556:130189.